## Slide 1
Tungsten Powder as an accelerator target
& In-Beam Testing
Ottone Caretta, Peter Loveridge, Tristan Davenne,
Mike Fitton, Joe O’Dell, Dan Wilcox and Chris Densham
(Apr. 4, 2013) (RAL)
Ilias Efthymiopoulos, Nikolaos Charitonidis
(CERN)
Funded by ASTEC, CERN subscriptions & PASI

## Slide 2: Davenne: Limitations of target technologies
Peripherally cooled monolith
Flowing or rotating targets
Segmented
Why powder?
Maintaining the target temperature and stress levels within safe limits is the main engineering design driver.
So designs become increasingly elaborate as energy and power deposited in the target are increased

## Slide 3: Candidate target technologies for a Neutrino Factory
1. Mercury
+ already exist, e.g. SNS
- toxic!
- reacts violently with beam
2. Moving Solid Tungsten Bars
+ studies on dynamic stress and strain-rate effects published
- Reliability in harsh environment?
- High static stress levels require much larger beam sigma than baseline beam parameters
3. Tungsten Powder
+ Pneumatic conveyance of powder demonstrated
- wear of parts and powder
- Containment
Mercury Jet in the MERIT experiment before (left) and after (right) a proton beam interaction, Kirk et al.
Pneumatically conveyed dense-phase tungsten powder jet, Caretta et al.
lifetime testing of tungsten wires in response to dynamic thermal loading, Skoro et al.

## Slide 4: Tungsten Powder Test Programme in PASI-WP3 + ASTEC
1
2
3
4
Offline testing
  Pneumatic conveying (dense-phase and lean-phase)
  Containment / erosion
  Heat transfer and cooling of powder
Unstable tungsten powder jet
High speed image: tungsten powder jet
High speed image: tungsten powder flow in a pipe
Dense-phase delivery
Lean-phase lift
Drag not what expected but at least it lifts!

## Slide 5: HiRadMat Beam Parameters: A high-intensity beam pulse from SPS of proton or ion beams is directed to the HiRadMat facility in a time-sharing mode, using the existing fast extraction channel to LHC. The SPS allows accelerating beams with some 1013 protons per pulse to a momentum of 440 GeV/c. Details of the primary beam parameters and focusing capabilities are summarised below: Beam Energy 440 GeV Pulse Energy up to 3.4 MJ Bunch intensity 3.0 · 109 to 1.7 · 1011 protons Number of bunches 1 to 288 Maximum pulse intensity 4.9 · 1013 protons Bunch length 11.24 cm Bunch spacing 25, 50, 75 or 150 ns Pulse length 7.2 µs Beam size at target variable around 1 mm2
In-beam experiment Opportunity, June 2012

## Slide 6: In beam test rig
Beam
LDV/camera
Lift Table
Tungsten powder sample in an open trough configuration
Helium environment
Two layers of containment with optical windows to view the sample
Remote diagnostics via LDV and high-speed camera
Open trough Assembly
Filling with Tungsten Powder
View from high speed camera
Beam
LDV/camera

## Slide 7: HiradMat Installation and Remote diagnostics

## Slide 8: HiRadMat: Run 7
Intensity: 8.40E+10 PoT

## Slide 9: HiRadMat: Run 8
Intensity: 1.75E+11 PoT

## Slide 10: HiRadMat: Run 9
Intensity: 1.85E+11 PoT

## Slide 11: HiRadMat: Run 21
Intensity: 2.94E+11 PoT

## Slide 13: Charitonidis
Trough photographed after the experiment. Note: powder disruption
Shot #8, 1.75e11 protons Note: nice uniform lift
Shot #9, 1.85e11 protons Note: filaments!
Lift height correlates with deposited energy

## Slide 14: Davenne: CFD predictions/post fits
CFD simulation of Shot #8, assuming 1 micron particle size (n.b. no lift with 25 micron particles at this intensity)
Test Results from Shot #8, 1.75e11 protons, beam sigma 0.75 mm x 1.1 mm
Beam heating
Average aerodynamic diameter ~30um

## Slide 15: Speculating (stumbling in the dark!)
1. EXTERNAL STRESS
A kick from the trough? Trough resonance perhaps too slow & Trough does not appear moving in the HSV
2. GAS LIFT
Lift proportional to Energy deposition CFD says yes but the energy/diameter is rather different. Drag model is incorrect for W or is it a different phenomenon?
3. THERMAL STRESS PROPAGATION
Lift proportional to Energy deposition Too slow and too late compared with propagation through a solid.
Peak ~40J/g (similar to MERIT) but 100 times lower velocities 0.5m/s.
Is this due to attenuation through the powder?
Chart: Displacement/time graph of RUN 8
| 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
height | 0 | 4 | 8.4 | 9.8 | 11.4 | 11.9 | 10.8 | 9.2 | 6.6 | 2.3 | 0.6
Chart: The first 40ms
| 0 | 2.5000000000000027E-3 | 5.0000000000000053E-3 | 7.5000000000000093E-3 | 1.0000000000000005E-2 | 1.2500000000000001E-2 | 1.5000000000000001E-2 | 1.7500000000000005E-2 | 2.0000000000000011E-2 | 2.2500000000000006E-2 | 2.4999999999999998E-2 | 2.7500000000000011E-2 | 2.9999999999999995E-2 | 3.2500000000000001E-2 | 3.4999999999999996E-2 | 3.7500000000000006E-2 | 4.0000000000000022E-2
 | 0 | 0.6 | 1.8 | 3 | 4 | 5 | 6 | 7.1 | 7.9 | 8.7 | 9.3 | 9.8 | 10.2 | 10.6 | 11.1 | 11.7 | 11.8

## Slide 16: LDV: the problems Part 1
No reliable beam stamp: the gitter
i.e. no measurement of stress wave propagation time!

## Slide 17: LDV: the problems Part 2
High frequency high amplitude noise?!
Yet not in all the runs?!
LDV vibration without beam

## Slide 18: LDV: the problems Part 3
Doom: watch out for the drift!
High vibration velocities before beam impact

## Slide 19: LDV: the good bits
Having taken all the bad data away (technically defined as data massaging!!)
the amplitude of vibration appears proportional to PoT
Vibration amplitude is higher in the inner trough than on the outer trough
There is a 1kHz resonant frequency peak (expected from trough resonance )

## Slide 20: Loveridge: ANSYS predictions
LDV data, filtered and offset corrected
<Shot #8, 1.75e11 protons, inner trough>
<Shot #9, 1.85e11 protons, outer trough>
Velocity ≈ 1 m/s
ANSYS simulation of secondary heat induced vibrations
Velocity ≈ 0.1 m/s
0 J/cc/spill
4.4 J/cc/spill
ANSYS vs LDV are “apart” by one order or magnitude

## Slide 21: Lessons learnt and stuff left to do
HiRadMat mark 2 (after CERN shutdown)
  Powder mono-size distribution
  More samples (prevent interference between measurements)
  Full length view of the sample
  Repeat test in He and vacuum (separate Aerodynamic Lift vs momentum transfer)
  LDV
    calibrate signal in situ
    use flat mirrors
    Establish beam gitter
    Watch out for windows interference
  Other general powder work
    Continue generic powder conveying study
    Calorimetric heat transfer
    Evaluate effect of magnetic field