## Slide 1: Study of a new high power spallation target concept
Yongjoong Lee
ESS, Materials, Target Division
5th High Power Targetry Workshop
May 20, 2014

## Slide 2: Spallation Target at ESS
5 MW spallation source
  5 MW (2.0 GeV/2.5 mA) proton beam
  2.86 ms long beam pulse with 14 Hz repetition rate
Rotating tungsten target:
  Helium cooled target with water cooled backup

## Slide 3: Motivation
Looking for a target concept that is based on simple design, with small number of standard type tungsten blocks in large dimensions.
Looking for a target concept that is based on simple cooling flow patterns such that CFD simulations have better predictability.
Demonstration of technical feasibility of a new target concept that is readily adaptable both for helium cooled and water cooled options.

## Slide 4: Target configuration used for this study
Five 40 cm long horizontal tungsten slabs with equal thickness 16 mm.

## Slide 5: Beam power deposition
TDR Baseline (2013):
  5 MW (2.5 GeV/2.0 mA) double Gaussian beam with peak current density 53 uA/cm2
Target volume | Deposited power [kW]
Target I | 820
Target II | 1374
Target III | 594
Total | 2788

## Slide 6: Flow analysis
Helium cooled option
  3 kg/s mass flow rate
  3 bar operation pressure
  Total 363 tungsten slabs
Water cooled option
  99 kg/s mass flow rate
  6 bar operation pressure
  Total 264 tungsten slabs

## Slide 7: CFD: Transient helium flow analysis
Helium Cooled Target |  |  | 
Target Volume | Max Temperature Pre-pulse | Max Temperature Post-pulse | Temperature Amplitude
Target I | 728.5 K | 813.9 K | 85.4 K
Target II | 736.0 K | 818.8 K | 82.8 K
Target III | 432.8 K | 450.9 K | 18.1 K
Pressure Drop | 97.0 kPa: Surface and time averaged |  | 

## Slide 8: CFD: Transient water flow analysis
Water Cooled Target |  |  | 
Target Volume | Max Temperature Pre-pulse | Max Temp: Post-pulse (Bulk/Surface) | Temperature Amplitude
Target I | 326.1 K | 429.7 K/393.6 K | 103.6 K
Target II | 334.3 K | 428.9 K/402.3 K | 94.6 K
Target III | 310.0 K | 329.4 K/324.8 K | 19.4K
Pressure Drop | 35.3 kPa: Surface and time averaged |  | 

## Slide 9: Stress analysis: Helium cooled target
Helium Cooled Target |  |  | 
Target Volume | Max Principal Stress Pre-pulse | Max Principal Stress Post-pulse | Stress Amplitude
Target I | 168 MPa | 194 MPa | 26 MPa
Target II | 116 MPa | 152 MPa | 36 MPa

## Slide 10: Stress analysis: Water cooled target
Water Cooled Target |  |  | 
Target Volume | Max Principal Stress Pre-pulse | Max Principal Stress Post-pulse | Stress Amplitude
Target I | 23 MPa | 113 MPa | 90 MPa
Target II | 26 MPa | 115 MPa | 89 MPa

## Slide 11: Decay heat analysis
Irradiation history: 5 years operation with 5000 hours per year beam on target at 5 MW
Benchmark (MCNPX): 41.5 kW in bare W at time zero
 | Dose rate calculated by FLUKA in kW |  |  |  |  | 
Cooling time [s] | 0 | 3600 | 7200 | 14400 | 28800 | 86400
He-cooled Naked W | 32.7 | 20.0 | 18.6 | 16.9 | 14.7 | 9.9
He-cooled 0.5 mm Ta-clad W | 39.3 | 25.9 | 24.3 | 22.7 | 20.7 | 16.1
H2O-cooled 0.5 mm Ta-clad W | 42.9 | 29.4 | 27.9 | 26.2 | 24.2 | 19.6
D2O-cooled 0.5 mm Ta-clad W | 39.9 | 26.6 | 25.0 | 23.4 | 21.4 | 16.8

## Slide 12: Decay heat analysis: Thermal equilibrium
Assumptions:
  Normalization factor in decay heat to make it total 47 kW
  Loss of coolant in the target and the monolith, with air ingression
Simple tungsten disc surrounded by monolith shielding blocks with 2 cm air gap between them.

## Slide 13: Decay heat analysis: Temperatures at thermal equilibrium
Coolant | Decay Heat at time zero | Decay heat at thermal equilibrium | Time to reach thermal equilibrium | Max. temperature at thermal equilibrium
Helium | 47 kW | 37 kW | 40 min | 912 K
Water | 62 kW | 38 kW | 270 min | 928 K

## Slide 14: Exothermic heat analysis
Tungsten and tantalum oxidation: exothermic process
  W + O2 -> WO2, dH = -589.7 kJ/W-mol
  W + 1.5*O2 -> WO3, dH = -842.9 kJ/W-mol
  Ta + 1.25*O2 -> 0.5*Ta2O5, dH = -1023.0 kJ/W-mol
Literature survey on tungsten and tantalum oxidation in air led to the estimation that the exothermic heat generated on the target surface will reach 10 kW at 800 C.

## Slide 15: Thermomechanical properties under flat proton beam profile
New accelerator baseline at ESS:
  Rastered beam scanning a rectangular surface on beam window: dx = 140 mm, dy = 32 mm
  Beam parameters changed from 2.5 GeV/2.0 mA to 2.0 GeV/2.5 mA, giving the peak current density on target 55.8 uA/cm2

## Slide 16: Evolution of target configuration – V2
Minimizing tungsten volume:
  No visible neutronic penalty by reducing the W slab length from 40 cm to 30 cm and the W slab total thickness from 80 mm to 70 mm
  Reduced W slab size reduces decay heat in W by more than 10 %.
  Optimizing temperature and stress configurations in W volume.
  No through going proton beam shall be allowed!

## Slide 17: CFD: Transient flow analysis – V2
Helium Cooled Target: 3 kg/s @ 6 bar |  |  | 
Target Volume | Max Temperature Pre-pulse | Max Temperature Post-pulse | Temperature Amplitude
Target I | 697.30 | 753.47 | 56.17
Target II | 714.59 | 800.82 | 86.23
Pressure Drop | 49 kPa: Surface and time averaged |  | 
Water Cooled Target: 99 kg/s @ 6 bar |  |  | 
Target Volume | Max Temperature Pre-pulse | Max Temp: Post-pulse | Temperature Amplitude
Target I | 320.11 K | 411.76 K | 91.65 K
Target II | 320.31 K | 417.21 K | 96.90 K
Pressure Drop | 34 kPa: Surface and time averaged |  | 

## Slide 18: Stress analysis: Helium and water cooled targets –V2
Helium Cooled Target |  |  | 
Target Volume | Max von-Mises Stress Pre-pulse | Max von-Mises Stress Post-pulse | Stress Amplitude
Target I | 99 MPa | 93 MPa | -6 Mpa (30 Mpa)
Target II | 68 MPa | 125 MPa | 57 Mpa (60 Mpa)
Water Cooled Target |  |  | 
Target Volume | Max von-Mises Stress Pre-pulse | Max von-Mises Stress Post-pulse | Stress Amplitude
Target I | 10 MPa | 70 MPa | 60 MPa
Target II | 12 MPa | 104 MPa | 92 MPa

## Slide 19: Thermal and mechanical analysis: Beam entrance window
Each of the 33 sectors could be considered as an 150 kW spallation target.
Maximum Temperatures in Beam Window |  |  | 
 | Pre-pulse | Post-pulse | Temp. Amplitude
Helium Cooled Target | 457.87 K | 485.71 K | 27.84 K
Water Cooled Target | 321.63 K | 351.49 K | 29.86 K
Maximum Stresses in Beam Window |  |  | 
 | Pre-pulse | Post-pulse | Stress Amplitude
Helium Cooled Target | 210 MPa | 280 MPa | 70 MPa
Water Cooled Target | 123 MPa | 153 MPa | 30 MPa

## Slide 20: Conclusions
The feasibility of the target concept based on sectorized horizontal slabs is demonstrated, both for helium cooled and water cooled options at 5 MW proton beam power.
Coolant | Number of W slabs | Max. Post-pulse temp. | Max. Post-pulse tensile stress | Max. temp. at LOCA
Helium 3 kg/s @ 6 bar | 495 bare W blocks | 801 K (528 C) | 125 MPa | < 639 C
Water 99 kg/s @ 6 bar | 495 Ta clad W blocks | 417 K (144 C) | 104 MPa | < 655 C
The exothermic heat generated from the oxidation of tungsten and tantalum could reach 10 kW at high temperatures above 700 C.
There are relatively small number of tungsten blocks in three standardized shapes.
The post pulse peak equivalent stress in the beam window is below 300 MPa both for helium cooled and water cooled options.

## Slide 21: Outlook
Next steps:
  Thermal and mechanical optimization
  Target vessel optimization
  Analysis of non-axisymmetric flux distribution
  Analysis of dynamic effects of the beam rastering
  Down to earth engineering and prototyping
Special thanks to Eric Pitcher, Per Nilsson and Thomas McManamy

## Slide 22: Open discussions
Thank you for your comments and feedback!