## Slide 1: Stresses and Deformations in 14 T Nb3Sn Solenoid of 0.8 m I.R. and 1.0 m O.R. & Half Length
Bob Weggel
10/7/10

## Slide 2
Hoop stress, σBjr = B jcoil r,
if each turn supported its own Lorentz force
Range −235 MPa (i.e., compression) to +926 MPa
Also, contour lines
Bz =14 T & 15 T
Cross section of upper half of Nb3Sn magnet with 0.8 m I.R. and 1 m O.R. & half length
Current density jcoil = 74.93 A/m2; central field B(r=0, z=0) = 14 T

## Slide 3: 1st principal stress, σφ, with isotropic winding pack Range = 250 to 476 Mpa, 51% the peak σBjr stress

## Slide 4: 2nd principal stress, σr Maximum magnitude ≡ σmax = 28 MPa, compression

## Slide 5: 3rd principal stress, σz σmax = 198 MPa, compression
.

## Slide 6: Von Mises ductile-material yield criterion, σvM ≡ sqrt{½ [(σφ−σr)2 + (σφ−σz)2 + (σr−σz2)]} Range = 250-598 MPa, 65% of the peak σBjr stress

## Slide 7: Deformation, exaggerated tenfold, with isotropic winding pack of 100 GPa Young’s modulus Range: 2.63-3.42 mm